## Slide 1: Chaos is cheap: adventures in nanomaterials synthesis
Sheryl Ehrman
Chemical and Biomolecular Engineering
University of Maryland, College Park
US Food and Drug Administration, April 16, 2015

## Slide 2: Outline
Chemical and Biomolecular Engineering at the University of Maryland
Overview of aerosol synthesis
Flame and solution CuO based photoactive nanoparticle materials
Concerns about environmental health and safety of nanoparticle based materials
Summary and outlook

## Slide 3: ChBE at the University of Maryland

## Slide 4: ChBE by the numbers
15 faculty, 2 assistant, 5 associate, 8 full professors
~ 340 undergraduate students with emphasis on undergraduate research experience
44 PhD, 18 MS students
~ 3 M external research expenditures FY 2013
CHBE Strengths: scholarly, entrepreneurial, diverse

## Slide 5: ChBE research interests
Transport phenomena, multiphase flow and process intensification
Processing of advanced materials for catalysis, energy conversion and energy storage applications
Biomolecular engineering
Systems engineering

## Slide 6: Current projects in the Ehrman laboratory
Aerosol synthesis of
  Lithium based oxide nanoparticles for battery cathode applications, collaboration with CS Wang, UMD
  Metal microparticles for printed electronics applications, collaboration with HD Glicksman, DuPont
Emissions and chemical transport modeling to support regional air quality improvement, collaboration with R. Dickerson, T. Canty, J. Stehr, UMD
Characterization of exhaled breath aerosols and respiratory protection, with applications to flu transmission, collaboration with D. Milton, UMD, Matthew Myers, Prasana Hariharan, Suvajyoti Guha, FDA

## Slide 7
10-10 10-9 10-8 10-7 10-6 10-5 10-4 10-3 10-2 10-2 10-1 1 10 100 1000
meters
http://farm4.static.flickr.com/3453/3276124739_e62fed7954.jpg
Fe nps
500 nm
Size selected Cu nps
Silver copper microparticles
Side view of film of TiO2 nps
What are nanoparticles and where are they found?
Notes: Benzene - ~ .7 nm, Nanometer to centimeter, wet or dry, AIChE Particle Technology Forum

## Slide 8: Example material: iron oxide
Size (< 10 nm) one magnetic domain per particle, superparamagnetic nanoparticles
MRI - positive (taken up by tissue of interest) or negative (not taken up) contrast
Many products in clinical use
Becomes part of normal iron load in body
More selective active targeting via surface modification an active area of research
B
Notes: T2 relaxation time shortening, caused by inhomogenaities in field around the particles. Feridex, IV taken up by healthy reticuloendothelial liver cells, allowing better view of tumors; Gastromark, oral, taken up in intestines, to allow better view of pancreas and other things near intestines

## Slide 9: Example products/future products
T2 Biosystems, US
http://www.nytimes.com/2009/08/30/business/30novel.html?_r=1&scp=1&sq=t2%20biosystems&st=cse
http://www.amagpharma.com/documents/products/pdfs/gastromark_insert.pdf

## Slide 10
Nanoproducts, consumer
  ©D. Hawxshurst/Wilson Center
  Safe handling of nanotechnology, Nature 444, 267-269 (16 November 2006)
  *http://www.nanotechproject.org/inventories/consumer/analysis_draft/

## Slide 11: Methods of making nanoparticles
Starting from molecular level
  From precursor
  Aerosol
    Combustion synthesis
    Thermal or plasma synthesis
  Solution phase synthesis
    Precipitation
    Sol gel
    Emulsion
  Evaporation/condensation
Starting from cluster level
  Spray pyrolysis
  Electrospray

## Slide 12: Nanoparticle engineering
System:
functionality
performance
Synthesis
Processing
Size
Shape
Crystallinity
Surface chemistry
Magneto, electro, optical properties…
Porosity, disperse/cohesive, retention or change of properties as synthesized…
Energy conversion efficiency
Catalytic performance
Sensor response
Rheological behavior…
Notes: Micro or nanoparticles part of a system which has functionality
Particle properties determine functionality
Processing, post processing modification determine properties

## Slide 13: Pros and cons
Rapid
Simple, less steps required
Product dry, no solvents
Amenable to continuous processing
May be scalable
Limited size control
Poor control of aggregation, especially gas to particle conversion
May battle thermodynamics in mixed systems
iron oxide/
silica

## Slide 14: Chaos is cheap, any proof?
From alibaba.com
Fumed silica (dry) as low
as $130/metric ton
Colloidal silica (30%) $600-$1000/metric ton
Fumed silica from our lab,
not for sale
Colloidal silica (stöber synthesis)
from our lab, not for sale

## Slide 15: Aerosol manufacturing, $$
Product | Volume, tons/yr | Market $/yr | Process
Carbon black | 8 M | 8 B | Flame
Titania | 2 M | 4 B | Flame
Fumed silica | 0.2 M | 2 B | Flame
Zinc oxide | 0.6 M | 0.7 B | Hot wall furnace
Fe, Pt, CeO2 | 0.02 M | 0.3 B | Hot wall furnace, spray pyrolysis
Ref: K. Wegner, S.E. Pratsinis, Chem. Eng. Sci. 51, 4581 (2003)

## Slide 16: Solar energy, the potential
http://www.nrel.gov/gis/images/map_pv_national_lo-res.jpg

## Slide 17
17

## Slide 18: Solar energy is intermittent
Storage of solar energy is key
Two approaches (of many):
Solar to electric to chemical energy
Photovoltaic (PV) + battery, supercapacitor, or…
Solar to chemical energy
Photoelectrochemical cells (PEC)
18

## Slide 19: Perspective
State of the art: solar to chemical
Khaselev and Turner, Science 280, 425 (1998)
12.4% efficiency

## Slide 20: Perspective: materials constraints
Semiconductor band gap of at least 1.4 eV required because of polarization, but should still absorb in the visible range ( < 2 eV)
Long electron-hole pair lifetimes
Stability in electrolyte
Efficiency and cost

## Slide 21: On a large scale, imagine….
J. Turner, Nature Materials, 7, 770-771 (2008)

## Slide 22: H2 as transportation fuel
The Hindu, 2 September, 2005
Bajaj Rickshaw Prototype
http://www.hinduonnet.com/2005/09/02/
stories/2005090204461400.htm
January 2012
15 H2 powered rickshaws
(Mahindra & Mahindra) deployed in New Delhi’s Pragati Maidan Exposition Center
A Yee, NY Times, Oct 1, 2012

## Slide 23: Perspective: life cycle
Efficiency
Cost

## Slide 24: Approaches to materials optimization
Start with highest efficiency, try to reduce costs, here, combination photovoltaic/ PEC device, NREL, eff: 12.4 %
Or… start with inexpensive materials and try to improve efficiency
Materials of interest include CuO, ZnO, TiO2
Khaselev and Turner, Science 280, 425 (1998)
Notes: Research Needs for the Hydrogen Economy say that no matter how cheap the PV or PEC material is, a minimum of 10% efficiency is needed because of unavoidable baseline costs of other system components
Definition of efficiency? The efficiency of H2 production was calculated
with the following equation: efficiency
5 (power out)/(power in). The input
power is the incident light intensity of 1190
mW/cm2. For the output power, assuming
100% photocurrent electrolysis efficiency,
the H2 production photocurrent of 120 mA/
cm2 is multiplied by 1.23 V, which is the
ideal fuel cell limit at 25°C (the lower
heating value of hydrogen). Calculated by
this method, the H2 production efficiency
of our system is 12.4% (24).

## Slide 25: Earth abundance
Atomic number, Z
http://pubs.usgs.gov/fs/2002/fs087-02/

## Slide 26: Favorable band edge position
0
-1.0
1.0
2.0
3.0
4.0
-2.0
ZnO
KTaO2
SrTiO3
TiO2
ZnS
CdS
CdSe
GaP
SiC
Si
MoS2
WO3
Fe2O3
3.4
3.2
3.2
3.2
3.6
2.4
1.7
2.3
3.0
1.1
1.8
2.8
2.3
Cu2O
CuO
2.0
1.7
H+/H2
O2/H2O
V vs. NHE (pH=0)
Band gap, eV
ZnO to Fe2O3 adapted from Navarro Y. et al., ChemSusChem. 2009; 2:471-485
Cu2O adapted from Gerischer H., Pure Appl. Chem 1980: 52: 2649-67
Notes: Cu2O are adopted from Gerischer, 1978,
Gerischer H. Heterogeneous electrochemical systems for solar energy conversion. Pure Appl Chem. 1980;52:2649-67.
and CuO are adopted from Chiang et al., 2012d

## Slide 27: Conversion efficiency
ηc | : | Solar to hydrogen conversion efficiency (%)
Io | : | Incident light intensity (W/m2)
jp | : | Photocurrent density at a certain applied voltage (mA/cm2)
E0rev | : | Standard water splitting reaction potential (1.23 V vs. NHE) at pH =0.0
Vbias | : | Applied external potential (V vs. RHE)

## Slide 28: CuO systems to date, low efficiency
System | Light source | Incident power density (W/m2) | Photocurrent density (mA/cm2) | Solar to H2 efficiency (%) | Reference
CuO | 500W Xenon | 1000* | 0.08 | 0.06* | Nakaoka et al., 2004
CuO | 150W Xenon Arc | 8100** | 2.2 | 0.20** | Chauhan et al., 2006
2% Li-CuO | 150W Xenon Arc | 8100 | 0.44 | 0.05 | Koffyberg and Benko,1982
* Assume to be 1000 W/m2
** Assume to be 8100 W/m2

## Slide 29: Photo - electro – chemical
material with
small bandgap
cell architecture
material with
right band position
cell architecture
light absorption
electron
separation
chemical
reaction
light
reflection

## Slide 30: Efforts to improve performance
Decrease particle size
(1)
Chiang et al., Int J H2 Energy, 2011
Increase conductivity
(2)
Chiang et al., J Electrochem Soc 2012
Increase porosity
(3)
Chiang et al., Int J H2 Energy 2012b
Shorten transport distance
(4)
Chiang et al., Nano Lett.
2012
Chiang et al., Int J H2 Energy, 2012a
light absorption
electron
separation
chemical
reaction
light
reflection

## Slide 31: Flame spray pyrolysis
compressed air
stir
nebulizer
burner
collector
filter
flame + particles
particles
vacuum pump
hood
precursor : copper nitrate
Powder/ethanol solution spin coated to form porous films, followed by heat treatment

## Slide 32: Processes occurring
coalescence
collision
condensation
single particles
aggregated
particles
chemical
reaction

## Slide 33
Particle morphology
Single Particles
Agglomerated Particles
tcoalescence < tcollision
tcoalescence > tcollision
Ulrich (1970’s), Helble, Sarofim (80’s), Friedlander, Koch, Windeler, Lehtinen (90’s)…

## Slide 34
burner
LNG
tunable angle
movable position
Control of particle size
w/o quenching
30% smaller
w/ quenching
Notes: 34

## Slide 35
H2
CuO
Pt
Ag/
AgCl
visible light
A
V
potentiostat
O2
PEC test station
150 W Oriel solar simulator + full reflector beam turning mirror, AM1.5G filter, incident intensity = 1 sun (1000 W/m2)
1M KOH electrolyte, pH 14
Notes: 150 W full spectrum solar simulator (Oriel Instruments, USA), coupled with a full reflector beam turning mirror (Oriel Instruments, USA) and a AM1.5G filter with
a measured intensity of 1 sun (1000 W/m2) by a reference cell (Oriel instrument, USA)

## Slide 36
Post processing treatment optimized
Spin coated films made from powder/ethanol
Scanning electron micrographs of samples sintering at different temperature and period: (a) 450 C for 1 h, (b) 450 C
for 3 h, (c) 600 C for 1 h, (d) 600 C for 3 h.
Solar to H2 efficiency 0.3%
Chiang et al., Int J H2 Energy, 2011
Chiang et al., Int J H2 Energy, 2012a
Notes: 36

## Slide 37
Precipitation route
Transmission electron micrographs of samples produced at (a) 25 C for 24 h, (b) 60 C for 45 min, (c) 95 C for 30 min
copper nitrate + NaOH
+ heat treatment 600 C,1 hour
Solar to H2 efficiency 0.7%
Chiang et al., Int J H2 Energy 2012b
Notes: 37

## Slide 38
Addition of Li to improve conductivity
SEM images of 2 at % Li doped CuO sintered at (a) 450◦C for 1 hr and (b) 600◦C for 3 hr.
Aqueous solution of copper nitrate + lithium acetate
Solar to H2 efficiency 1.3 %
Conductivity CuO only: 2 x 10−6 to 4 x 10−6 S/cm
with 2% Li 7 x 10−5 to 3 x 10−4 S/cm
Chiang et al., J Electrochem Soc 2012
Notes: Conductivity measured using electrical impedance spectroscopy
38

## Slide 39: Additional structures
Polycrystalline
film
Polycrystalline nanorod
Single crystalline nanowire
Current collector + polycrystalline
3.2 % efficiency

## Slide 40: 55 gallon drum of silicon tetrachloride vs fumed silica
https://www.khlubes.com/images/55_gallon_drum.jpg
silica
surface area = 1.6 m2
surface area = 2.4 x 107 m2
assuming 300 m2/g

## Slide 41: Potential risks associated with engineered nanomaterials
Exposure opportunities over the life cycle of the nanomaterial, intended, unintended
  Raw materials
  Manufacturing
  Use
  Disposal/reclamation

## Slide 42: Routes for exposure, intentional or unintentional
Dermal
Gastrointestinal
Inhalation
Toxicity measurements in animals
LD50 = dose required to kill 50% of a population of test animals (mg/kg)
OSHA Permissible exposure limits (PELs) in humans, 8 h time weighted average (mg/m3)
Size of material considered in some cases,
ex: respirable quartz, but no separate standards for nanomaterials
Notes: Dermal: resistance: Stratum corneum, keratinized dead skin cells and lipds
GI: uptake of neutrients by willi/micro villia in intestines
Lung : alveolar membrane/blood

## Slide 43: MSDS info on titania, not nano
Cas: 13463-67-7
RTECS #: XR2275000
Name: TITANIUM DIOXIDE. MOLECULAR FORMULA: TIO*2. MOLECULAR WEIGHT: 79.9.
OSHA PEL: 15 MG/M3
*PEL 8 hour time weighted permissible exposure limit
https://fscimage.fishersci.com/msds/23510.htm
5 nm particles have 100 x
the surface area per gram
as 500 nm particles
~ 275 x EPA 24 h standard for 2.5 micron diameter or less particulate air pollution

## Slide 44: Primary pathways hypothesized at the cellular level
Particle surface/cell interactions cause oxidative stress, increased intercellular calcium and gene activation
Transition metals from NPs cause same
Cell surface receptors are activated by transition metals from NPS leading to gene activation
NP/mitochondria interactions cause oxidative stress
Figure in Oberdoerster et al., Environmental Health Perspectives, 113, 823-838 (2005)
Adapted from Donaldson and Tran Inhal. Toxicol. 14 5-27 (2002)
Notes: Formation of free radicals, accumulation of peroxidative products, depletion of antioxidants

## Slide 45: Response in rats and mice correlates well with surface area, for inhaled engineered NPs
Oberdörster G, Philos Trans R Soc Lond A 358(2000) 2719–2740
Oberdörster et al., Environ. Health Perspectives, 113 (2005) 823-839

## Slide 46: Not just surface area
Free silanol group intensity
Pandurangi et al., Environ Health Perspect 86: 327-36 (1990)
Ability to catalyze reactive oxygen species formation in vitro
Limbach et al. Environ Sci Tech 41: 4158-4163 (2007)
…..
No generalized trends have emerged across all material systems
What about combinations of nanoparticles with other substances?

## Slide 47: Real exposure scenarios - may not be single component
Other components physi- or chemisorbed to the engineered nanomaterial surface
  Nanoparticle based targeted therapeutics
  Consumer product formulations
  Accidental release of nanoparticles together with condensable or reactive species
  Nanoparticles modified by environment between release and exposure

## Slide 48: Our testable hypothesis
Initially non-toxic nanoparticles may serve as carriers of toxic compounds into biological systems
Adverse effects may correlate with nanoparticle specific surface area
Image: http://www.php4windows.com/Articles/trojan_horse_in_business_home_software.jpg

## Slide 49: Testing this hypothesis, system components
Relatively non-toxic ubiquitous nanoparticles
  Fumed silica, Aerosil
  Evonik, ~ 50 through 350 m2/g specific surface area
Low molecular weight water soluble (~ 2.4 g/L) toxic molecule, cisplatin
Positive control, quartz, ~ 1 micron mass median diameter
Cell line, bovine chondrocytes
Notes: Quartz - known carcinogen, generates reactive oxygen species

## Slide 50: About cisplatin
Potent antitumor agent used to treat different type of cancers
Cytotoxic mode of action
  Interacts with DNA
  Forms intra-strand cross-linkages
  Leads to activation of apoptosis
Cisplatin and some other chemo agents adversely effect skeletal system of children, thus effects on chondrocytes previously studied
Cl
Cl
NH2
H2N
Pt

## Slide 51: Experimental approach
Attachment of toxin (cisplatin) to non-toxic (fumed silica) surface
Characterization of the surface modified silica particles
in vitro tests on chondrocytes
  Membrane integrity via fluorescence microscopy using the Live/Dead (calcein/ ethedium bromide) stain
  Metabolic function via the MTT (methylthiazol tetrazolium) assay
  Electron microscopy
Notes: 3-(4,5-dimethylthiazol-2-yl)-2,-diphenyltetrazolium bromide

## Slide 52: Attachment of cisplatin to silica
O
NH2
+
~
O
O
~
Si
Cl
Cl
NH2
H2N
Pt
+
Silica
APTES
NH
Cl
NH2
NH2
Pt
O
O
~
Si
O
~
Aminopropyl
triethoxysilane
under N2
2% v/v APTES in acetone, overnight, room temperature
under N2 overnight, room temperature
Cisplatin

## Slide 53: Fluorescence microscopy, Live/Dead stain
50 mm
negative control
Aerosil 380 only
Aerosil 380+ cisplatin
positive control
5 mg/ml free cisplatin
positive control quartz
50 mm
50 mm
50 mm
24 hrs exposure
Notes: Top left, control
Top right, aerosil 380 = cisplatin alone
Bottom left, cisplatin alone, 5 micrograms/ml
Bottom right, quartz

## Slide 54: MTT assay
Cell culture wells washed, then 300 µl of MTT solution (0.5 mg/ml) added
Plates incubated at 37 0C for 2 hrs allowing for reduction of tetrazolium salt to a formazan (blue) dye by active mitochondria of the cells
300 µl of solubilizing buffer (10% Triton X 100 with 0.1N HCl in anhydrous isopropanol) added to dissolve the formazan
Absorbance was measured at 570 nm using microplate reader

## Slide 55: MTT results, silica/cisplatin
*
*
*
*
*
*
*
*
*
*
*
*
*
*
*
*
Error bars represent standard deviation of four replicates
Asterisks denote statistically significant (p < 0.05) differences between experiment and control

## Slide 56: Correlation
R2 = 0.61
R2 = 0.76
R2 = 1.0

## Slide 57: Transmission electron microscopy comparison to control…
b
Qualitative observations
- intracellular particles observed in both
- nuclei more compact in control sample
Notes: Looked at 50-100 cells from each sample

## Slide 58: Discussion
Free cisplatin can enter cells by active and passive transport
Adverse effects on cell function may result from
  cells internalizing particles/cisplatin (true trojan horse)
  particles releasing
  cisplatin near the
  cell membranes

## Slide 59: Discussion
Metabolic function correlated negatively with surface area
Fluorescence imaging indicates significant adverse effects on cell membranes and DNA
Effects comparable to free cisplatin at 5 mg/ml
No synergistic adverse effects observed, nor did silica mitigate effects of cisplatin on cells
TEM images show the particles are inside the cells
Adverse effects on cell function may result from transport of cisplatin near cells or directly into cells by particles

## Slide 60: Take home message
May not be enough to consider nanoparticles by themselves when examining effects of engineered nanoparticles on biological systems
Must evaluate potential for co-release with other compounds, reactive or condensable, that may be hazardous
Must evaluate fate of nanoparticles in the complex environment after release

## Slide 61: Acknowledgements
+ NIST
Dr. Peter Zavalij
Dr. Karen Gaskell
Dr. Li-Chung Lai
Nick Franson
Kosi Aroh
Yoon Shin
Chia Ying Chiang
Jillian Epstein, REU student
Dr Tridib Bhowmick, Dr. John Fisher
Fishchell Department of Bioengineering